## Slide 1
Bio-orthogonal catalysis for cancer therapy
Shreyas Wagle
ESR 2 Fellow
Institution: Tel Aviv University
Group: Organic & Polymer chemistry
Supervisor: Prof. Roey J. Amir
E-mail: wagle@tauex.tau.ac.il
Mid-Term Check Meeting
Edinburgh, 5th June 2019

## Slide 2
Personal Trajectory
B.Tech Textile Chemistry
Fibre Sciences
Organic chemistry
Internship at BASF(India)
Pigment Printing
Stretchable Prints
Bachelor Thesis
Synthesizing nanocellulose
Superabsorbent Films
Internship at Vishnu Dyeing and Printing
Pre-treatment Layout
Dyeing & Printing layout
M.Sc. Polymer Material Sciences
Polymer Chemistry
Polymer Physics
Research Project
Synthesis of self-healing probes
Encapsulation of the chemical probes
PhD Micellar Catalysts
Design & synthesis of multi-functional polymeric amphiphiles.
Catalytic activation of anti-cancer prodrugs.
M.Sc. Master Thesis
Optical damage sensing and self-healing system

## Slide 3
Background & skills
Institute of Chemical Technology, Mumbai (India)
Martin Luther University, Halle (Saale), (Germany)
Polymer Chemistry,
Organic Synthesis
Fluorogenic Probes
Textile Chemistry
Fibre Sciences

## Slide 4
Research project
Foreseen research
Amphiphilic block copolymers with mono/bivalent ligands
Catalysis experiments
Structure Activity studies & formulation optimization
Objectives
Develop block-copolymer amphiphiles bearing mono or bivalent ligands
Metal complexation and self-assembly of micelles
Characterization of Structure activity relationship of (nano)catalysts and its optimization

## Slide 5
Scheme
R = Alkyl chain (length= 6,7,8,12)
Cell internalization studies

## Slide 6
Tests | Measurements
GPC | 1.054
DLS | 20 ± 3.0 nm
CMC | 4±2 µM
Tests | Measurements
GPC | 1.039
DLS | 32 ± 6 nm
CMC | 3±1 µM
Tests | Measurements
GPC | 1.044
DLS | 30 ± 3 nm
CMC | 4±1 µM
Tests | Measurements
GPC | 1.034
DLS | 24 ± 1 nm
CMC | 4±2 µM
PEG-C7 Hybrid
PEG-C8 Hybrid
PEG-C12 Hybrid
PEG-C6 Hybrid
Preliminary Results

## Slide 7
Preliminary Results
mPEG-Lys(Boc)-fmoc
mPEG-Lys(Boc)-BU
mPEG-Lys(Boc)-4xC12
Sample | PDI
mPEG5k-OH | 1.036
mPEG5k-NH2 | 1.051
mPEG5k-Lys(B)-BU | 1.040
mPEG5k-L(B)-4xC12 | 1.039
Chart: Dh(nm)
32 ± 6 nm

## Slide 8
Secondments
Secondment 1
Institution and sector: Stratingh Institute for Chemistry, Rijksuniversiteit Groningen (Academic)
Duration: 3 months
Main research objectives: Metal catalyst synthesis
New knowledge and competences expected to be acquired: Organometallic Chemistry, Catalyst Synthesis, structure characterization, catalysis performance and profile.
Secondment 2
Institution and sector: Tagworks Pharmaceuticals BV (Non-academic)
Duration: 4 months
Main research objectives: In-vivo micelle imaging
New knowledge and competences expected to be acquired: In vivo chemistry, Radioimmunoimaging, PET imaging, Start-up development

## Slide 9
Scientific and Transversal Skills Training
Local training
Synthesis & characterization of micelles
Courses
Chemistry of Sugars
Methods & tools in chemical Biology
Synthesis & characterization of ligands and their complexes
ICS 2019
Exploring metal catalysis
New cancer treatment pathways
Preliminary Catalysis
Using polymer encapsulated complex for catalysis
NMR
HPLC
TEM

## Slide 10
Scientific and Transversal Skills Training
PhD studies
University: Tel Aviv University, Israel.
Title of PhD: Micellar catalysts
Enrolment: 21/11/2018
Network-wide training
Training event at TU/e (03/‘19)
Introduction to programme
Scientific communication
MTC Meeting(06/‘19) & Bioorthogonal & Bioresponsive 2019
Discussion with Project officer
Bio-orthogonal chemistry symposium
Training event at Basel (09/’19)
Chemical synthesis & catalysis
Prodrugs: design principles, synthesis
ICCA conference(09/’19)
Catalysis and Chemical Engineering
Secondment at RUG
(Early 2020)
Catalyst Synthesis
Catalyst performance & profile
Training event at Edinburgh(2020)
Designing delivery systems
in-vitro imaging and cell assays
Training event at Tel Aviv (2021)
in vivo imaging
In vivo chemistry and cancer biology
Training event at Barcelona (2021)
Career opportunities in industry and interview simulations
Innovation and Entrepreneurship